CUSTOMER:	ABB

1/2

DATA SHEET

GPN: EMVY630GRA221MKE0S (Invest. No.: G110260A0394D1)

DIMENSIONS (unit: mm)

0.20max

| Case code |  D | L | A | B | C | W | P |
| --- | --- | --- | --- | --- | --- | --- | --- |
| KE0 | 12.5 | 13.5 | 13.0 | 13.0 | 13.7 | 1.0 to 1.3 | 4.2 |

Remark:	Sn100% plating of lead wire

# LIST OF STANDARDS

(1)	Rated DC Working Voltage:		63V

(2)	Nominal Capacitance:			220µF			at 20°C and 120Hz

(3)	Operating Temperature Range:	-40°C to +105°C

(4)	Capacitance Tolerance:			-20% to +20%		at 20°C and 120Hz

(5)	Leakage Current:				less than 138µA		at 20°C, after 2 minute

(6)	Dissipation Factor:			less than 0.14		at 20°C and 120Hz

(7)	Impedance:					less than 0.19Ω		at 20°C and 100kHz

(8)	Ripple Current:				max. 500mArms		at 105°C, 100kHz

| (9) | Low Temperature Characteristics: | Z(-25°C)/Z(20°C) = 2 |
| --- | --- | --- |
|  | (Max. impedance ratio at 120Hz to the 20°C value ) | Z(-40°C)/Z(20°C) = 3 |

| (10) | Load Life: | The following specifications shall be satisfied when the capacitors are restored to 20°C after rated DC voltage is applied for 5,000 hours at 105°C. |
| --- | --- | --- |

- Capacitance change		 20% of the initial value

- Dissipation Factor		 200% of the initial specified value

- DC Leakage current		 The initial specified value

| (11) | Shelf Life: | The following specifications shall be satisfied when the capacitors are restored to 20°C after exposing them for 1,000 hours at 125°C without voltage applied. |
| --- | --- | --- |

- Capacitance change		 20% of the initial value

- Dissipation Factor		 200% of the initial specified value

- DC Leakage current		 The initial specified value

2/2

DATA SHEET

GPN: EMVY630GRA221MKE0S (Invest. No.: G110260A0394D1)

(12) 	Recommended Reflow Profile (One reflow only)

| Series / Size | Preheat | Pb-free type |  |  |
| --- | --- | --- | --- | --- |
|  |  | Time over 217°C | Time over 240°C | Peak temp. |
| MVY / 63V KE0 | 150-200°C 60 - 180 seconds | 50 seconds max. | 20 seconds max. | 245°C max. |

Note:			- Dissipation Factor	 120% of the initial specified value after 1 x soldering

- ΔL				 0.9mm after soldering